## Slide 1: VirtualBatteryFoam: A Multi-physics Numerical Solver to Simulate the Aluminium Electrolysis Varchasvi Nandana, Roman Gutt, Hendrik Gesell, Alessandro Cubeddu, Roman Duessel, Uwe Janoske 27.02.2019 Chair of Fluid Mechanics Bergische Universität Wuppertal
Notes: Represent the chair of fluid mechanics of wuppertal, espacialy the Aluminium Electrolysis team, involved people (read names)

## Slide 2: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis
27.02.2019
Conventional industrial cells are designed for constant power
Shift towards renewable sources of energy demands
  Process flexibility
  Production efficiency
Notes: Current is supplied to the cell over the busbar system into the Steel rod -> fork -> carbon anode, surrounded by electrolyte (cryolite), ->aluminium -> cathode -> collectorbar -> next cell
Cryolite low conductivity -> Aluminium high conductivity -> Most of voltage drop inside electrolyte
Low conductivity cryolite -> Joule Heating -> Liquid Cryolite , Aluminum (660°C)
Ledge -> Solid cryolite at wall -> Protects the insulation
Frequently insert aluminum oxide -> reacts with anode -> CO2 + Aluminum is produced.
Right now conventional cell -> constant current
Goal -> Process flexibility -> stabelize power supply -> flexibility sometimes more important than efficiency

## Slide 3: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis as virtual battery
Power variation in
Grid
Anode to cathode distance (ACD)
Shell heat exchanger
27.02.2019
Notes: Problems involved from flexible current supply -> heat generated -> Increase Current -> Joule heating -> control -> ACD + SHE -> ledge thickness

## Slide 4: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis
Reducing cell voltage leads to magneto-hydrodynamic instabilities!!
Aluminium Electrolysis as virtual battery
27.02.2019
Notes: High current -> Induced magnetic field ->High Lorentz -> Disturbs ->Aluminium contact with anode
Conclusion reducing voltage -> mhd instasbilities

## Slide 5: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: A complex problem
27.02.2019
Notes: Many physical phenomenas are involved

## Slide 6: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis
Magnetohydrodynamics
Bubble dynamics
VirtualBatteryFoam: A multi-physics tool
Thermoelectric
Turbulent heat transfer
27.02.2019
Notes: 4 submodel -> 1 final model

## Slide 7: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Magnetohydrodynamics
Metal Pad Rolling
Current takes the least resistance path
Horizontal component of current reacts with vertical magnetic field to produce Lorentz force
The interface begins to rotate
27.02.2019

## Slide 8: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Navier-Stokes
VoF
U,p,γ
Elec. Potential
Elec. Potential
𝛻∙(𝜎𝛻ϕ)=𝛻∙𝜎(𝑢×𝐵)
Current density
Current density
𝐽=𝜎(−𝛻ϕ+𝑢×𝐵)
magn. potential
A(r)
magn. potential
A(r)=µ/4π ∫17_𝑉▒〖𝐽(𝑟^′ )/|𝑟−𝑟^′ |^ 𝑑𝑉(𝑟^′ ) :𝜕Ω 〗
−∇^2 𝐴= 𝜇𝐽 :Ω
Lorentz force
Lorentz force
𝐹_𝐿=𝐽×𝐵
magn. Field
magn. Field
𝐵=∇×𝐴
Navier-Stokes
VoF
U,p,γ
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019

## Slide 9: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
1: Side walls, 2: Copper anode plate, 3: 900 Steel electrodes, 4: Liquid metal (InGaSn), 5: Steel cathode plate, 6 und 7: electrical connections
Pedchenko Experiment
Pedchenko, S. Molokov, J. Priede, A. Lukyanov, and P. J. Thomas, Experimental model of the interfacial
instability in aluminium reduction cells," EPL (Europhysics Letters), vol. 88, p. 24001, Oct 2009.
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019
Notes: Immersed into liquid

## Slide 10: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019

## Slide 11: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019

## Slide 12: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Complete cell geometry
Structured mesh (10.000.000 Cells)
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019

## Slide 13: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Static electric field
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019
Notes: 14 Region

## Slide 14: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Influence of magnetic field from the neighhbour cells
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019
Owner: A() =
Neighbour: A() =

## Slide 15: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
X-component
Y-component
Z-component
upstream
without neighbour
with neighbour
Magnetic flux with and without the neighbour cells
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019

## Slide 16: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Velocity field with and without the influence of neighbour cells
without neighbour
With neighbour
Aluminium Electrolysis: Magnetohydrodynamics
27.02.2019

## Slide 17: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: mass transfer and bubble dynamics
During aluminum reduction process, gas (mainly CO2) is produced at anode surfaces:
Gas production and gas dynamics disturb the interface electrolyte /aluminum
Gas layer under anodes introduces additional voltage drop
Target
Study gas production and gas dynamics
Optimize the cell geometry to reduce gas effects
27.02.2019
Notes: CO2 low conductivity -> Voltage drop -> efficiency lost -> fast transport of CO2 out of system.
Study gasdynamics , Gas production

## Slide 18: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: mass transfer and bubble dynamics
27.02.2019
Multiphase fluid dynamics problem involving:
electrochemical production of aluminum and gas
mass transfer and mass change (electrolyte  gas)

## Slide 19: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
 | Sim | Zhao et al.
Release frequency [s] | 21.5 | 21.5
Max coverage [%] | 97.8 | 98-99
Zhibin Zhao et al., Anodic bubble behavior and voltage drop in a laboratory transparent aluminum electrolytic cell, Met and Mat Trans B Vol 47, Issue 3, June 2016, 1962-1975
Aluminium Electrolysis: mass transfer and bubble dynamics
27.02.2019

## Slide 20: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Solidification (Ledge)
Porosity-Enthalpy method in VOF framework to capture formation of ledge
Joule energy ( ) is modelled as explicit volumetric source term
Melt fraction,
Energy conservation equation:
Momentum switchoff using Darcy type source term:
27.02.2019
Solidification source

## Slide 21: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
V. Nandana and U. Janoske, Experimental and numerical study on the melting behaviour of a phase change material in buoyancy driven flows, 7th European Conference on Computational Fluid Dynamics, Glasgow, 2018
Aluminium Electrolysis: Solidification (Ledge)
27.02.2019
Schematic
Experiment
Simulation

## Slide 22: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Solidification (Ledge)
27.02.2019
Temperature distribution
Ledge profile for different line currents
Thermal field and ledge profiles

## Slide 23: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Shell heat-exchanger
Approach to model reduction
Simulation of wall cooling with full resolved shell heat-exchangers not feasible
Reduction of SHE to wall heat flux boundary conditions
Temperature distribution in the cell
Temperature distribution in SHE
27.02.2019
Notes: 44 SHE -> seperated -> use as BC

## Slide 24: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Heat transfer enhancement
27.02.2019
Augmentation can be achieved by disrupting the boundary layer
Longitudinal vortices cause mixing and enhanced heat transfer
Passive methods to enhance heat transfer rates
  Winglets
Notes: Incease heat transport forced convection -> disrupting boundary layer -> enhanced heat transfer due to vortices -> Passive method -> winglet -> after winglet longitudinal vortice

## Slide 25: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Numerical approach for scientific studies
27.02.2019
OpenFOAM® Version 4.0
Turbulence model RANS k-𝜔-SST
Divergence schemes second order
Solver rhoSimpleFoam
  Semi-structured mesh of single delta winglet
6.5 M cells (single) – 21 M cells (array)
Resolved wall boundary layer
  Max
  Average
Mesh independency of results proved via three different mesh densities
Notes: Sience fine mesh , Industrial coarse mesh

## Slide 26: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
  G. Zhou & Q. Ye, Experimental investigations of thermal and flow characteristics of curved trapezoidal winglet type vortex generators, Applied Thermal Engineering, Vol. 37, 2012
Smooth channel
Channel with winglet
27.02.2019
Aluminium Electrolysis: Shell heat-exchanger

## Slide 27: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: Shell heat-exchanger
27.02.2019
Qualitative distribution of surface heat flux at cell walls
Streamlines with temperature prolie
Notes: Redirected 90° -> several winglets

## Slide 28: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Heat flux vs wall temperatures
Aluminium Electrolysis: Shell heat-exchanger
27.02.2019
Notes: Main take away easy to control -> linear -> good to control ledge thicknes

## Slide 29: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Conclusions
Implementation of the numerical solver “VirtualBatteryFoam” presented.
The long wave instability is simulated and validated with experiments from Pedchenko et al.
The production of CO2 and its dynamics comprising of coalescence, build-up and release is compared with the experimental results of Zhao et al. and was shown to be in good agreement.
The solidification model is validated with experimental results.
Fully resolved shell heat-exchanger simulations are carried out for model reduction of cell wall cooling
27.02.2019

## Slide 30: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Future work
Implement a model for transport and dissolution of alumina
Couple heat transfer with solidification and MHD model
Extend the solver to include magnetisation effects of the steel shell
Validate the fully integrated model with industrial measurements.
27.02.2019

## Slide 31: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis
Conferences
V. Nandana and U. Janoske, Experimental and numerical study on the melting behaviour of a phase change material in buoyancy driven flows, 7th European Conference on Computational Fluid Dynamics, Glasgow, 11-15 June 2018.
R. Gutt, V. Nandana, U. Janoske, A Numerical Study of Metal Pad Rolling Instability in a Simplified Hall-Héroult Cell, 7th European Conference on Computational Fluid Dynamics, Glasgow, 11-15 June 2018.
H. Gesell, V. Nandana, U. Janoske, Numerical investigation of the heat transfer characteristics of new winglet shapes in three-dimensional turbulent flows, 12th European Fluid Mechanics Conference, Vienna, Austria, 11th September 2018.
V. Nandana, R. Gutt, A. Cubeddu, R. Duessel, U. Janoske, A multi-physics numerical solver to simulate the aluminium electrolysis process, ICSOBA 2018, Belem, Brasil, 1st November 2018.
A. Cubeddu, V. Nandana, U. Janoske (2019). A numerical study of gas production and bubble dynamics in a Hall-Héroult reduction cell. Proceedings TMS 2019 Annual Meeting & Exhibition, San Antonio, Texas, USA.
Journal
V. Nandana, U. Janoske, Numerical study on the enhancement of heat transfer performance in a rectangular duct with new winglet shapes, Thermal Science and Engineering Progress 6 (2018) 95 – 103. doi:https://doi.org/10.1016/j.tsep.2018.03.005.
H. Gesell, V. Nandana, U. Janoske, Numerical study on the heat transfer performance and efficiency in a rectangular duct with new winglet shapes in turbulent flow, International Journal of Heat and Mass Transfer [in review].
27.02.2019

## Slide 32: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Acknowledgements
This research was funded by the German Ministry of Education and Research under the project “SynErgie” (No. 03SFK3B1), whose support is gratefully acknowledged.
The authors would also like to thank the continuous support and cooperation of TRIMET Aluminium SE, Essen, Germany.
Additionally, the support of European Regional Development Fund (ERFE.NRW) and the state of Nordrhein-Westfalen through the projects “Aluminium Electrolysis 4.0” and “FlexTherm” is gratefully acknowledged.
The authors are grateful for the infrastructural support of the HPC cluster "Pleiades" at the University of Wuppertal.
27.02.2019

## Slide 34: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: mass transfer and bubble dynamics
27.02.2019
Mass transfer  Faraday’s law
[kg/s]
where
I – current passing through electrode (kA)
M – molar mass of the substance (g/mol)
F – Faraday constant (C/mol)
Z – valency number
Electric current  Gauss`s law
=0
Where
is the electrical conductivity (S/m) and
is the potential drop (V)

## Slide 35: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Aluminium Electrolysis: mass transfer and bubble dynamics
27.02.2019

## Slide 36: VirtualBatteryFoam: A multi-physics numerical solver to simulate aluminium electrolysis
Where
indicates a pair of phases (e.g. electrolyte/gas)
represents the interface forces between phases (like: lift, drag, virtual mass, wall lubrication, etc.)
where is sum of drag, lift and virtual mass forces
Aluminium Electrolysis: mass transfer and bubble dynamics
27.02.2019
Multiphase fluid dynamics  Euler-Euler method
Momentum equation
Volume Fraction conservation
  Aluminium and bath as continuous phase
  Gases as dispersed phase
  Each phase has its own mass and momentum conservation equation